## Slide 1
2020 Postdoc Research Day Presentation Conference
M. Bulut Coskun
Organization: 389R
Advisor: Mina Rais-Zadeh (389R)
Postdoc Program: JPL
Single Pixel
Sparse Data Collection
Sparse Array of Pixels
Reconstructed IR Image
IR Imaging using Sparse Microresonator Arrays and Compressed Sensing
Data Recovered
(90% of the pixels are missing)
IR Radiation Sensitive
Microresonator

## Slide 2
Introduction
Easier signal routing
and densely placed pixels
Reduced power
consumption
Less complex
electronics
at the expense of moderate post-processing time.
(b) Why Sparse Arrays?
Sparse sensor arrays, by definition have reduced number of elements enabling,
The project aims to develop an instrument capable of taking infrared (IR) images in harsh environments (high radiation and high temperatures up to 500°C) using a sparse array of resonant-based micromechanical devices.
(a) The Ultimate Goal:
(c) Outline:
Pixel design
Sparse array construction
Compressed sensing
Test and recovery procedure
Results
Discussion and future work
1

## Slide 3
Pixel Design
Analysis of the Thermal Design Parameters
Meandering Tether Design provides higher:
Thermal Resistance,
Sensitivity, and
NETD.
Total Length (μm) | 28.5 | 76.5
Ther. Resistance (K/W) | 9146 | 24519
Time Constant (μs) | 201 | 540
Parameter | Description | Value
Lr ­ | Resonator Length | 60 μm
wr | Resonator Width | 30 μm
tr | Resonator Thickness | 4 μm
L1 L2 Wt Qan | Tether Length 1 Tether Length 2 Tether Width Anchor loss limited Q | 4.5 μm 15 μm 3 μm 1.29 x107
Straight Tether
Meandering Tether
Finalized Design Parameters
Tether geometry affects both mechanical and thermal parameters.
Tether Optimization to Maximize the Q-Factor
High-loss design
Losses minimized via FEA
Length Extensional Mode: fres = 57.1 MHz
GaN
2

## Slide 4
Sparse Array and Compressed Sensing
Here the goal is to use the incomplete data obtained from m number of resonators (pixels) and recover the complete image comprises n pixels, where n >> m.
Sparse Pixel Array
The problem can be mathematically formulated as an underdetermined system of equations as follows:
ymx1 = Φmxn xnx1
Collected Sparse Data
Measurement Matrix
Data to be recovered
A solution can be obtained by min‖x‖1 s.t. y = Φ x
To guarantee the existence and uniqueness of the solution, X has to be sparse, and Φ has to satisfy the Restricted Isometry Property (RIP).
  X can be transformed into a different domain, where it is sparse (e.g. FFT, DFT etc.).
  Randomly constructed measurement matrices have a high probability to satisfy RIP.
Matrix Representing the Array Layout
1
1
1
1
0
0
0
0
0
0
0
0
0
0
0
0
3

## Slide 5
Pixel Fill Factor (FF) and Image Preprocessing (STEPS 1-2)
FF=0.1
Test and Recovery Procedure
STEP 1
Test Image (TI) is obtained. (credit:NASA/JPL)
384x384
FF=0.11
128x128
STEP 2
Downscaled the TI to take the fill factor into account.
STEP 3
Construction of the sparse array, and Φ.
Sparse Data Collection
(128x128 array with 25% density )
STEP 4
l1-magic toolbox is used to reconstruct the image.
4

## Slide 6
Arrays with Different Densities
Array Density (%) | Correlation Coefficient | Recovery Error
10 | 0.9045 | 0.19
25 | 0.9629 | 0.12
37.5 | 0.9785 | 0.08
Performance Metrics
“1” represents a perfect positive correlation, and “0” indicates no correlation.
Test Image
5
Sparse Data Collection by 128x128 Arrays
Reconstructed Images
Density: 10%
Density 10%: Outlines around the large and medium sized features are distinguishable. Acceptable correlation coefficient. Relatively high error.
Density: 25%
Density 25%: Improved clarity on small and medium sized features, and substantial increase in the correlation coefficient.
INCREASING ARRAY DENSITY
Density:37.5%
Density 37.5%: Smaller details are revealed, the edges get sharper and correlation coefficient and the recovery error are further improved.

## Slide 7
Conclusion and Future Work
Case 2
Density: 10%
Test Image
Constructed Images
Case 1
Recovery Error | 0.19 | 0.08
Correlation Coef. | 0.9045 | 0.9653
Future work
Future work will focus on fabrication, and characterization of the proposed arrays.
6
Additional Discussion:
Publication:
M.B. Coskun, M. Rais-Zadeh, “IR Imaging using Sparse Microresonator Arrays and Compressed Sensing”, in preparation for The 34th International Conference on Micro Electro Mechanical Systems (IEEE MEMS 2021).
Reported performance metrics are image-dependent, hence the recovery performance can be substantially improved, while working on a test image with large features and less details.
Increasing the array size, while keeping the density the same, also yields improved performance for the given field of view (FOV).